Magnesium diboride (MgB2)
Conventional superconductor with special features
  - double gap model
  - highest Tc among BCS superconductors (39K)

---
MgB2 thin films
Two samples (#2, #3) out of three have undergone neutron scattering:
  - destroys anisotropy
  - makes film properties similar to a single-gap BCS superconductor

---
BCS model predictions
Single gap, plus a phenomenological parameter (Dynes' Γ)

---
BCS model predictions

---
Double gap
DoS (hence, dI/dV) as a linear combination of two single-gap Densities of States
  - “normalized” coefficients απ + ασ = 1
  - w/ constraint 0.66 < απ < 1

---
Computational difficulties
- The conductivity curve depends non linearly on Γ and Δ through a numerical integral (no analytical solution)
- Double-gap model leads to five independent parameters: Γπ, Δπ, Γσ, Δσ, and one coefficient e.g. απ

---
Finding the best fit (method 1)
Simplex
  - most powerful method, with limitations
  - doesn't need derivatives
  - χ² is “yet another function” to find a minimum for
  - can't estimate statistical errors

---
Finding the best fit (method 2)
gsl_multifit_*()
  - not a generic minimization procedure
  - less robust than Simplex on “irregular” functions but...
  - ...can estimate statistical covariances and sigmas!
  - min χ²(Γπ, Δπ, Γσ, Δσ, απ) Levenberg-Marquardt

---
Best of both worlds?
- Simplex method to find a good minimum
- Starting from the last result, gsl_multifit_fdfsolver_iterate() to (slightly) improve the fit, but most importantly compute statistical errors

---
https://www.youtube.com/watch?v=LLLq7-0DivI
https://bitbucket.org/gderosa/didvsuperc/src

---
Results
Sample #1; single gap
  - Γ	= 0.2639±0.0023
  - Δ	= 2.2327±0.0023
  - χ²/DoF	= 17.669

---
A better fit with a double gap
Sample #1; double gap
  - Γ	= 0.1866±0.0019
  - Δπ	= 1.7895±0.0050
  - Δσ	= 3.2348±0.0073
  - απ	= 0.6660±0.0027
  - χ²/DoF	= 3.4737

---
The single gap model fits better with “disordered” (neutron-scattered) films
Samples #2 and #3, single-gap first (Γ, Δ), then double-gap (Γπ, Δπ, Γσ, Δσ, απ)

---
Results